Supplying 100mm inside dia best quality uPVC roof grade soil pipe BRB -D/ AZIZ (1st one is 1st preferable if unavailabe of 1st one than 2nd one & 3rd one wil be used gradually), under the pipe will be soling & 3" C.C. casting having specific gravity 1.35-1.45, water absorption for 24 hrs 0.1% wall thickness 2.7mm-3.4mm , heat reversion at 1500c, the change is <5% for 15 minutes & 60 minutes immedrsion time for oil bath & air oven respectively, resistant to acetone, opacity <0.2%, break at elongation, rigidity, elasticity, tensile streess, bending stress, compressive stss, impact stress at 230c are >80%, 1.12x10.4kg/cm2, 2600-3000kg/cm2, 45-55mm2, 21kg/cm2, 600-700kg/cm2, 1-2ft. ibs/in and 0.5-1ft.ibs/in of notch respectively, hydrostatic pressure for 1hr is 310 psi, propet eletic, thermal, flow, chemical resistance fitted and fixed in position with sockets, bends (National Polymer (NPI/Azz/Zakaria Polymer) with all accessories such as found gratting/domes roof gratting bands, sockets (Brand mentioned will be selected by sanctioning authority/engineer-in-charge.