50mm dia G.I. pipe with wall thickness 3.65mm, outside diameter min 59.7mm, weight 5.38kg/m, can with sand min 50 kg/cm2 hydraulic pressure.