40mm dia G.I. pipe with wall thickness 3.25mm, outside diameter min 47.9mm, weight 3.83kg/m, can with sand min 50 kg/cm2 hydraulic pressure.