20mm dia G.I. pipe with wall thickness 2.65mm, outside diameter min 26.5mm, weight 1.70kg/m, can with sand min 50 kg/cm2 hydraulic pressure.