Supplying best quality uPVC roof grade T.S pipe BRB / Aziz (1st one is 1st one preferable if unavailable of 1st one than 2nd one & 3rd one will be used gradually), having specific gravity 1.35-1.45, water absorption fo r 24 hrs 0.1% wall thickness 2.7mm -3.4mm, heat reversion at 1500c the change is <5% for 15 minutes & 60 minutes immersion time for bill bath & air oven respectively, resistant to acetone, opacity <0.2%, break at elongation, rigidity, elasticity, tensile stress, bending stress, compressive stss, impact tress at 230c are >80%, 1.12x10.4kg/cm2, 2800-3000 kg/cm2, 45-55kg/cm2, 21kg/cm2 600-700 kg/cm2 1-2ft. ibs/in and 0.5-1ft.ibs/in of notch respectively hydrostatic pressure for 1hr is 310 psi propet eletic, thermal, flow, chemical resistance fitted and fixed in position with sockets, bends (Nationel Polymer (NPI/Azz/Zakia Polymer) with all accessories such as round gratting/domed roof gratting bands, sockets (Brand mentiond will be salected by sanctioning authority/engineer-in-charge.