**Procedure of providing Tack coat on road**:

60/70 grade bitumen (From Eastern Refinery Ltd) will be heated on a temperature of 151-161 degree Celsius. 0.732 kg bitumen will be spread over the perfectly cleaned per sqm road uniformly in heated condition.