**Seal Coating:**

For a good finished, levelled, cambered and sloped surface (compacted thickness) premixed consolidated seal coating, filler materials pea gravels and Sylhet sand (FM 2.5) is to be mixed thoroughly for obtaining the required grading which should be free from any dust, organic matter, clay and any other objectionable matter premixed with heated (121 to 155 degree Celsius) bitumen (60/70 grade from Eastern Refinery Ltd) @99 kg per cum mixture of pea gravels and sand heating at mixing temperature 135 to 163 degree Celsius (aggregate temperature 150 to 163 degree Celsius) in/c loading of aggregates with gauging box (0.625 cft) made of wood or steel into the mixing pan. The mixed materials shall be laid to a uniform 12mm thickness, rolled with 8-10 M ton road roller by 8-10 times on every single point as soon as possible and before the mat cooled down to a temperature of 107C to have perfectly compacted road.